## Slide 1
List three advantages of using LLDPE over LDPE.
(B) List at least 4 reasons why PE is the material of choice for these types of containment vessels
PQ5 Polymer Question 5
(A) LLDPE give Higher tensile strength, impact and puncture resistance
and lower thickness (gauge) films can be blown with environmental
stress cracking resistance compare to LDPE.
Answer
(B) PE is a thermoplastic thus easily mouldable allowing a wider variety of shapes to be made. The material is cheap as is the ease of manufacture.
It has low Tm and Tg so is tough and is impact resistant and good chemical resistance.

## Slide 2
PQ6 Polymer Question 6
As can be seen from material selection chart, there are many options for a low pressure gas pipe based on your performance index. Comment on why the final selection is based on PE by considering other selection criteria for the other polymeric, metallic and ceramic materials.
Answer
The ceramics are below the line having very low a toughness. The metals need expensive fittings or costly joining techniques. Metals have also low chemical stability. Polymers of which the most commonly used is PE offer a suitable choice for a large low pressure gas distribution network as it is a low temperature thermoplastic and thus can be welded easily.

## Slide 3
PQ7 Polymer Question 7
A “Yield before break” or ductility factor is used as material performance index to prevent plain strain fracture in polymer. Using a suitable equation derive a yield before break performance index and use this Table, to rank these polymers.
Answer
Polymer | K1C | σy | Ductility factor
PE | 5.0 | 15.8 | 31.9 mm
PP | 3.5 | 16.4 | 14.5 mm
PVC | 4 | 54.0 | 1.7 mm
The highest is PE followed by PP and then PVC
PE PP PVC

## Slide 4
PQ8 Polymer Question 8
Extrusion is an example of an important processing method for
polymers. Explain how the screw speed influence the effectiveness of the extrusion process.
Answer
If screw speed too fast - insufficient residence time to melt the polymer, can lead to melt fracture as a result of instability due to slip of the melt at the die walls. This leads to roughened surfaces, “sharkskin surfaces”
If screw speed too slow - excessive temperatures through viscous heating will degrade the polymer by oxidation.